Semi-automatic blowing machine

Model: YC-2L-2

| Main machine (blow molding part + oven) | Model type | YC-2L-2 |
| --- | --- | --- |
| Product Spec | Max. product volume(L/cav) | 2 |
|  | Max. preform neck size(mm) | 50 |
|  | Max. product diameter(mm) | 90 |
|  | Max. product height (mm) | 360 |
|  | Cavities | 2 |
| Blow molding part | Die force (KN) | 120 |
|  | Die stroke (mm) | 120-210 |
|  | Max. mould size（mm） | 390*345 |
|  | Mould thickness | 120-160/220-270 |
|  | Mould spacing（mm） | 120-170 |
|  | Max. pulling stroke（mm） | 340 |
|  | Operation pressure(Mpa) | 0.8-1.0 |
|  | Operation air pressure consumption (1tr/min) | 300 |
|  | Blow pressure(Mpa) | 1.2-2.8 |
|  | Blow air pressure consumption (1tr/min) | 350 |
|  | Output（pcs/h） | 1500-1800 |
|  | Machine size（LxWxH）(m) | 1.46*0.58*1.8 |
|  | Package size （LxWxH） | 1.66*0.77*2.12 |
|  | Machine weight(KG) | 650 |
| Oven | Temperature grade（rate） | 6 |
|  | Heating time（S） | 90-200 |
|  | Voltage（V） | 220 or as your request |
|  | Frequency（HZ） | 50 |
|  | Total power（KW） | 6.3-10.3 |
|  | Actual power consumption（KW） | ≤5 |
|  | Oven Size （LxWxH） | 1.35*0.55*1.15 |
|  | Package size （LxWxH） | 1.55*0.75*1.35 |
|  | Oven weight (KG) | 300 |

| Auxiliary device | Required Spec | YC-2L-2 |
| --- | --- | --- |
| High pressure air compressor | Operation air pressure | 3.0 Mpa |
|  | Air displacement | 0.75 m3/min |
|  | Power | 9 Kw |
|  | R.P.M | 800 |
|  | Weight | 460 Kg |
|  | Dimension | 1.86m*0.9m*1.4m |
| Air filter (oil-water separator ) | Filter precision | ≤5ppm |
|  | Weight | 28Kg |
|  | Dimension | 0.24m*0.26m*0.73m |

| Air compressor |  |
| --- | --- |
| Air filter |  |

| Other configuration ways about the type YC-2L-2 |
| --- |
| Blow molding part (set) | Oven (set) | Use condition | Remark |
| 1 | 1 | Standard configuration | Any type |
| 1 | 2 | Thick preform which heating time is long |  |
| 2 | 1 | Thin preform which heating time is very short (normally the volume under 400ml) | Increase the air compressor displacement up to 1.2m3/min |